10. Preparation for Film Sample

Put the film sample on the electronic scale;

Read the sample’s mass;

Take the tray with the film sample out of the electronic scale;

Cut about “5 cm” length Kapton tape with “5 mm” width（it is not too wide）;

Leave about “1 cm” of distance to one end of the tape,

Make that the sample is flush with the tape;

Take the sheet-shaped sample chamber,

Ensure that the upper edge of tape is closely stuck to the upper positionof the flat surface of the sample chamber (as shown in the video);

At the same time, both ends of the sample should be equal to the margins ofthe sheet-shaped sample chamber, and ensure that the film sample is in the middle of sample chamber (as shown in the video);

Then press the tape tightly against the sample chamber;

Tighten the tape up;

The preparation of the film sample is finished.